## Slide 1
Machinability Analysis in Ball End Milling of Ti6Al4V Alloy
LAV KUMAR SINGH (221030012009)
MAHAK CHAUHAN (221030012010)
MOHAMMAD UMAR (221030012011)
JATIN GURJAR (221030012008)
Advance Manufacturing Project:-
Dr. Mithilesh Dikshit
Course Co-ordinator

## Slide 2
Introduction
Titanium alloys are widely used in aerospace, biomedical, and automotive industries due to their exceptional strength-to-weight ratio, high corrosion resistance, and excellent biocompatibility. However, these properties also pose significant challenges during machining, such as high cutting temperatures, rapid tool wear, and poor machinability.
This analysis focuses on understanding the performance of ball end mills in machining titanium alloys. It evaluates :-
  TOOL WEAR (Upto Vc i.e.0.3mm)
  Surface Roughness
  Power
under fix operating conditions including Cutting speed, feed rate, and depth of cut.

## Slide 3
Ti-6Al-4V
Ti-6Al-4V is the most commonly used titanium alloy, accounting for over 50% of all titanium alloy applications. Its popularity spans industries like aerospace, medical, automotive, and
marine due to its :-
  High strength-to-weight ratio
  Corrosion Resistance
  Biocompatibility
Machining Challenges
  Low thermal conductivity
  Increased Ductility
  Rapid tool wear
Fig. 1

## Slide 4
  Tool Geometry: Ball end mills feature a hemispherical tip that enables
multi-axis machining of complex 3D surfaces.
BALL END MILLING
  Diameter: Cutting Diameter of 8 mm.
  Material: Tungsten carbide (providing Durability, resistance to wear at high temp.)
  Surface Finish: Produce Smooth finishes on 3-d surfaces
  Helix Angle: 30° helix angle, providing a balanced combination of cutting performance and smooth material removal.

## Slide 5
Ball End Mill Tool
VMC Machine
Fig. 2
Fig. 3

## Slide 6
Machining
1- Process Parameter :-
  Feed per tooth : 0.05 mm/tooth
  Depth of cut : 0.8 mm
  RPM: 4380
2-Process Parameter :-
  Feed per tooth : 0.2 mm/tooth
  Depth of cut : 1.1 mm
  RPM: 6000
Fig. 4

## Slide 7
Tool Maker Microscope
Taylor Hobson S-128 Surface Roughness Tester
Instruments Used
Fig. 6
Fig. 5

## Slide 8
  Observation Table

## Slide 9
  Observation Table

## Slide 10
Length(in mm)
Tool Wear(in mm)
Tool Wear vs Length

## Slide 11
Length(in mm)
Surface Roughness(in mm)
Surface Roughness vs Length

## Slide 12
Length(in mm)
Power Consumption(in kVA)
Power Consumption vs Length

## Slide 13
Tool Wear upto Vc(0.3 mm)
Fig. 8
Fig. 7

## Slide 14
Conclusions
From the experimental view on the ball end milling ofTi-6Al-4V alloy, the following conclusions were drawn:
  Tool Wear of 0.1mm (Va) is observed at length 30mm (After 3 slots)
  Tool Wear of 0.2mm (Vb) is observed at length 80mm (After 8 slots)
  Tool Wear of 0.3mm (Vc) is observed at length 120mm (After 12 slots)
  Peak of Power is observed at Va.

## Slide 15
Thankyou